Herefordshire Model – MAC Service information Baseline Specification for Highway Works – Public Realm Services


Herefordshire Model - MAC Contract 

SERVICE INFORMATION - ANNEX 25 – BASELINE SPECIFICATION FOR HIGHWAY WORKS

PUBLIC REALM SERVICES

APPENDIX 0/2

CONTRACT-SPECIFIC MINOR ALTERATIONS

TO EXISTING CLAUSES, TABLES AND FIGURES INCLUDED IN THE CONTRACT

CONTENTS AMENDMENT SHEET

	Issue

No.
	Revision

No.
	Amendments
	Initials
	Date

	01
	00
	First issue
	
	

	
	
	
	
	

	
	
	
	
	

	
	
	
	
	

	
	
	
	
	

	
	
	
	
	


	APPENDIX 0/2:
	CONTRACT-SPECIFIC MINOR ALTERATIONS TO EXISTING CLAUSES, TABLES AND FIGURES INCLUDED IN THE CONTRACT

	List of Alterations to Existing Clauses, Tables and Figures



	Clause No
	Title

	
	

	
	SERIES 100:PRELIMINARIES

	114
	Payment Applications

	
	

	
	SERIES 600:  EARTHWORKS

	602
	General Requirements

	TABLE 6/1
	Acceptable Earthworks Materials: Classification and Compaction Requirements

	TABLE 6/2
	Grading Requirements For Acceptable Earthworks Materials

	
	

	
	SERIES 800:  ROAD PAVEMENTS – UNBOUND, CEMENT AND OTHER HYDRAULICALLY BOUND MIXTURES

	802
	Transport, Laying, Compaction and Trafficking of Unbound Mixtures

	803
	Type 1 Unbound Mixtures

	
	

	
	SERIES 900
ROAD PAVEMENTS - BITUMINOUS BOUND MATERIALS

	903
	Placing and Compaction of Bituminuos Mixtures

	
	Compaction

	
	Joints

	
	

	
	SERIES 3000:  LANDSCAPE AND ECOLOGY

	3001
	General

	3002
	Weed Control (Selective Weed Control in Grass)

	3004
	Ground Preparation

	3005
	Grass Seeding, Wildflower Seeding and Turfing

	3006
	Planting

	3007
	Grass, Bulbs and Wildflower Maintenance

	3009
	Establishment Maintenance for Planting

	3010
	Maintenance of Established Trees and Shrubs


	SERIES 100:
	PRELIMINARIES

	
	

	Clause 114 Payment Applications

	
	Delete the heading of Clause 114 and Sub Clause 114 (1).

	
	


	SERIES 600:
	EARTHWORKS

	
	

	Clause 602 General Requirements

	
	

	
	Table 6/1:

	
	Delete Classes 4 and 6B.

	
	Add the classes in the following addendum to Table 6/1 (material properties required for acceptability are given in Appendix 6/1).


Addendum to TABLE 6/1  ACCEPTABLE EARTHWORKS MATERIALS

	Class
	General Material Description
	Typical Use
	Permitted Constituents
	*1
	Compaction Requirements in Clause 612

	4A
	Granular material
	Fill to landscape areas
	Any natural material.
	
	Clause 620

	4B
	Cohesive material
	Fill to landscape areas
	Any natural material.
	
	Clause 620

	5E
	Sub-soil
	In lieu of  topsoil
	Any natural sandy sub-soil excavated from defined limits within the works
	
	As for Class 5A and 5B

	6B
	Selected coarse granular material
	Stabilisation of formation and starter layer
	Crushed cobbles and gravel crushed non-argillaceous rock, crushed concrete or recycled aggregate.
	
	Table 6/4

Method 5

	6F2
	Selected coarse granular material
	Slope stabilisation

Cut/fill transition

Blinding to Class 6B

Capping layer
	Any crushed natural material other than argillaceous rock. Crushed concrete or recycled aggregate.
	
	Table 6/4

1. Method 2

2, 3 and 4.  Method 6

	6N
	Selected

well graded granular material
	Fill to structures

Face drainage/slope stabilisation treatment
	Any crushed natural material other than argillaceous rock. Crushed concrete or recycled aggregate except recycled asphalt.
	
	1. End product, 95 % of max dry density determined by the alternative vibratory hammer method in App 6/1.

2. Table 6/4 Method 2

	6N1
	Selected

uniformly graded granular material
	Granular bed beneath bank seat foundations for integral structures
	Uncrushed natural gravel. 10 mm single size to BS 882
	
	Table 6/4  

Method 3

	8A
	Cohesive fill
	Lower trench fill in drainage
	Any natural cohesive material. No stones or gravel > 37.5 mm BS sieve
	
	Table 6/4  Method 1

	8B
	Well graded fill
	Lower trench fill in drainage
	Any natural well graded material.

No stones or gravel > 37.5 mm BS sieve
	
	Table 6/4  Method 2

	8C
	Uniformly graded fill
	Lower trench fill in drainage
	Any natural uniformly graded material. No stones or gravel > 37.5 mm BS sieve
	
	Table 6/4  Method 3


Column annotated *1 is as per the column of the SHW Table 6/1, Material Properties Required for Acceptability (In Addition to Requirements on the Use of Fill Materials in Clause 601 and Testing in Clause 631).
	
	

	
	Table 6/2 Add the Classes in the following table.

	
	

	
	Addendum to TABLE 6/2  GRADING REQUIREMENTS FOR ACCEPTABLE EARTHWORKS MATERIALS




	
	Percentage by mass passing the size shown

	
	BS Sieve Sizes

	CLASS 
	150 mm
	125 mm
	75 mm
	50 mm
	37.5 mm
	20 mm
	10 mm
	2 
mm
	80 µ
	63 µ

	4A


	
	
	
	
	100
	
	
	
	
	0-25


	SERIES 800: 
	ROAD PAVEMENTS – UNBOUND, CEMENT AND OTHER HYDRAULICALLY BOUND MIXTURES

	
	

	Clause 802 Transport, Laying, Compaction and Trafficking of Unbound Mixtures

	
	Sub-clause 1, after the first paragraph add the following paragraph:

	
	

	
	Moisture content to remain within the range 1% above to 2% below the optimum moisture content determined in accordance with the Vibrating Hammer Method test in BS 1377: Part 4 and without drying out or segregation.

	
	

	Clause 803 Type I Unbound Mixtures

	
	Sub-clause 1:

	
	

	
	After "crushed rock" delete the “crushed slag, crushed concrete, recycled aggregates or well burnt non-plastic shale and may contain up to 10% by mass of natural sand that passes the 4mm test sieve".

	
	and 

	
	after "crushed rock" insert “crushed concrete or recycled aggregate".


	SERIES 900: 
	ROAD PAVEMENTS - BITUMINOUS BOUND MATERIALS

	
	

	Clause 903  Compaction

	
	Sub-clause 18:

	
	After “decks”:- delete the full stop and add the following “and urban residential areas.”

	
	

	Clause 903  Joints

	
	Sub-clause 21:

	
	Add the following to the end of the existing sub-clause:-

	
	“Transverse joints in surface courses, excluding thin surface courses to Clause 942, shall be saw cut. The width of any binder film on the surface course, resulting from longitudinal joint coating, shall not exceed 25 mm. Where binder films exceed 25 mm the Provider shall, undertake measures to ensure that the Skidding resistance value of the film is at least equal to the value on the adjacent completed surface course, for the affected length.”

	
	

	
	Sub-clause 22:

	
	Delete existing sub-clause (iii)

	
	Delete existing sub-clause (iv)


SERIES 3000 LANDSCAPE AND ECOLOGY
3001 General

Quality Management Systems

3001.2
Sub Clause 2 line 2
Insert ‘working’ before ‘hours’

Pesticide Applications

3001.7
Sub-Clause 7, paragraph 2, line 6

After: ‘Environment Agency‘

Add: ‘and the Service Manager’

3002
Weed Control

General

3002.1
Sub-Clause 1, Paragraph 1

Delete: ‘required in the locations and at the frequencies given in Appendix 30/2’

Insert: ‘in accordance with Defra guidelines ‘Guidance on the disposal options for common ragwort’ and ‘Guidance note on the methods that can be used to control harmful weeds’ and ‘The Weeds Act 1959’
3002.2
Sub-Clause2

Delete existing sub-clause 

Add: ‘Weed control shall be to the following standard as stated in Appendix 30/2.’

Total Weed Control

3002.3
Sub-Clause 3, line5

Delete: ‘at the locations and frequency stated in Appendix 30/2’ 
Insert: ‘all of the Public Realm’

3002.4
Sub-Clause 4 line 4

Delete: ‘at the locations and frequency stated in Appendix 30/2’  

Insert: ‘to the areas as stated on the Service Order’

3002.5
Sub-Clause 5, line 4

Delete: ‘at the locations and frequency stated in Appendix 30/2’ 

Insert: with ‘to the areas as stated on the Service Order’

Selective Weed Control in Grass

3002.6
delete Sub-Clause 6

3002.9
delete Sub-Clause 9

3004 Ground Preparation

Vegetation Clearance

3004.1
Sub-Clause 1, line 1

Delete: ‘Where stated in Appendix 30/4’ 

Insert: ‘Where stated in a Service Order’

3005 Grass Seeding, Wildflower Seeding and Turfing

Establishment Cuts

3005.29
Sub-Clause 29 

Delete sub-clause:

Add new sub-clause:

‘Newly-established grass, whether newly-sown or turfed, shall be mown to leave a nominal height as stated in Table 30/2. The first mowing shall be carried out once the grass has reached a height of 100 mm. Any turves disturbed by mowing shall be re-firmed into their original position and watered to their full depth.’

3005.30
Sub-Clause 30 

Delete sub-clause

Add new sub-clause:

‘Arisings from grass cutting shall be dealt with as shown in Table 30/2’

3006 Planting

Plants

3006.7
Sub-Clause 7, line 1

Insert at start ‘On request’

3007 Grass and Bulbs

General Grass Maintenance

3007.3
Paragraph 3, line 1

Delete: ‘at the frequencies and to the heights specified in this Clause’ and Insert: ‘in accordance with Table 30/2’

3007.8 
delete sub-clause 

Grass Cutting: High Frequency

3007.9 to 3007.12

Delete sub-clauses 

Grass Cutting: Medium Frequency

3007.13 to 3007.16


Delete sub-clauses 

Grass Cutting: Low Frequency

3007.17
delete sub-clause

Grass Cutting: Minimal Frequency

3007.19
Sub-Clause 19, line 1

Delete: ‘1m’ 

Insert: ‘1.2m’

3007.20
delete sub-clause 

Grass Cutting: Banks and Ditches

3007.22
delete sub-clause 22

Grass Cutting: Areas of Planting

3007.23 to 3007.25

Delete sub-clauses

3009 Establishment Maintenance for Planting
Stakes, Tubes Guards and their Ties

3009.3
Sub-Clause 3, line 2

Delete: ‘twice per year on October and March,’

Pruning

3009.7
Sub-Clause 7, line 2

Delete: 300mm

Insert: 500mm

Weed Control : Young Trees and Shrubs in Cultivated Beds

3009.16
Sub-Clause 16, line 1

Delete: ‘Where required in Appendix 30/9, planting areas shall be visited monthly to carry out specified weed control operations’

3009.18
Sub-Clause18, line 4

Delete: ‘at least once a year’

Weed Control: Hedges

3009.21
Sub-Clause, line 2

Delete ‘once per year in March’

3009.22
Sub-Clause 22, line 

Delete: ‘Where sheet mulch has been laid, it shall be inspected three times per year’’

3009.25
Sub-Clause25

Delete sub-clause

3010
Maintenance of Established Trees and Shrubs

Weed Control: Trees and Shrubs in Cultivated Beds

3010.2
Sub-Clause 2, line 2 

Delete: ’four times per year’

3010.2
Sub-Clause 2, line 9

Add at end of existing sub-clause: ‘or within 30 days of initial treatment’

Shrub Pruning

3010.8
Sub-Clause 8, item (i), line 3

Delete: ‘as stated in Appendix 30/10’

Hedge Maintenance

3010.12
Sub-Clause 12, line 2

Delete: ‘The frequency and timing shall be as given in Appendix 30/10’

3010.14
Sub-Clause 14, line 

Delete ‘highway’

PAGE  
February 2012 – V1.00

154




